Beijing Kinghey International Trade Co., Ltd.

Silver Coated Aluminum Powder

| Silver-coated aluminum powder using advanced technology coating silver, abtain the uniform layer of silver at the surface of aluminum beads.This product is a perfect combination of the high conductivity, the high shielding effectiveness of silver and the cheap aluminum powder，instead of the pure silver powder is one of the best materials to achieve a very high price. This product is mainly used for electromagnetic compatibility requirements of the terminal device, 20% silver content especially suitable to meet the requirements of 83528 rubber conductive filler. |
| --- |
| Typical Properties Product Morphology Ag ( % ) Power Resistivity mohms-cm Particle Size ( um ) Scott Apparent Density ( g/cm3 ) D10 D50 D90 SA60S20 Sphere 20 0.7 45 60 75 1.53 SA40S20 Sphere 20 1.2 25 40 55 1.51 SA30S20 Sphere 20 1.2 15 30 55 1.50 |
| Application fields ●Conductive silicone rubber; ●Conductive adhesive; ●Conductive paint. |  |
| Attention ●The products in the packaging intact, under normal storage conditions for one year shelf life; ●Products should be placed on ventilation, dry place, anti-sun, rain, damp, to avoid bulk package; |